## Slide 1: Spin wave excitations in Fe on the basis of band theory
Blackman, J. A., Morgan, T. & Cooke, J. F. Prediction of High-Energy Spin-Wave Excitation in Iron. Phys. Rev. Lett. 55, 2814–2817 (1985).
Theory:
Mook, H. A. & Nicklow, R. M. Neutron Scattering Investigation of the Magnetic Excitations in Iron. Phys. Rev. B 7, 336–342 (1973).
Experiment:

## Slide 2
270
255
Paweł Buczek, Arthur Ernst, and Leonid M. Sandratskii. Different dimensionality trends in the Landau damping of magnons in iron, cobalt, and nickel: Time-dependent density functional study. PhysRevB.84 (174418) (2011).
75
Time dependent DFT calculations

## Slide 3: Comprehensive measurements of SW excitations in Fe in Ei 200-1400meV using TOF spectrometer (MAPS)
[1+x,1+x,0]
E meV
[x,0,0]
[0,z,0]

## Slide 4: No evidence of Stoner Continuum gap anywhere in whole 80-200 meV range
May be some evidence for gap in [1,0,0] direction.
(DFT predicted?)
Intensity along dispersion
curve
Fitted dispersion
|D|=230 [meV*A-2]
[0,z,0]
Gap?
[x,0,0]
[0,z,0]
[x,0,-1]
[x,0,0]
E meV
E meV
I (arb. units)